Certificate of Analyses

27.02.2025

PineChemical Group Oy

Helsinki, Finland

Crude Tall Oil

Date of Production: 26.02.2025

Container no: GPLU4260584

Net weight: 21 725 kgs

| ### Properties | ### Standard | ### Analysis |
| --- | --- | --- |
| ### Appearance | ### Brown or dark brown color oily liquid |  |
| ### Acid Number, mg of KOH per 1 g of product, min | ### 96 | ### 101.9 |
| ### Unsaponifiables Matter, % wt., max | ### 25 | ### 23.8 |
| ### Water, %, max | ### 2 | ### 1.9 |
| ### Mass fraction of rosin acids not more than, % | ### 18 | ### 9.3 |

PineChemical Group OY representative					            Natalia Sokolova