Certificate of Analyses

20.05.2025

PineChemical Group Oy

Helsinki, Finland

Tall Oil PITCH (TOP KOR)

Specification: Technical specification 16217983-006-2018

Date of Production: 19.05.2025

Container no: KRIU2262908

Net weight: 22 410 kgs

Confirmation no: CF25040006 dd 25.04.25

Delivery date: 06 June 2025

| ### Properties | ### Standard | ### Analysis |
| --- | --- | --- |
| ### Acid Number, mg of KOH per 1 g of product, max | ### 70 | ### 43 |
| ### Softening point, °C, min | ### 19 | ### 34 |
| ### Viscosity, c | ### - | ### 58 |

Guarantee shelf life is 6 months from the date of production.

PineChemical Group OY representative					            Natalia Sokolova