Certificate of Analysis

01.07.2025

PineChemical Group Oy

Helsinki, Finland

Tall Oil Pitch (TOP SEG)

Specification: Technical specification 51321438-010-2022

Date of Production: 17.04.2025

Container no: EXFU5637075

Net weight: 21 700 kgs

Contract: Agreement №2 to the Supply agreement №11/03/2025

| ### Properties | ### Standard | ### Analysis |
| --- | --- | --- |
| ### Acid Number, mg of KOH per 1 g of product, min | ### 20 | ### 71 |
| ### Loading temperature, °C |  | ### 105 |
| ### Dynamic viscosity, Pa*s |  | ### 0.355 |
| ### Softening temperature, °C, not less | ### 19 | ### - |
| ### ASH, % max | ### 0.5 | ### 0.1 |

Guarantee shelf life is 12 months from the date of production.

PineChemical Group OY representative					Natalia Sokolova