Certificate of Analysis

28.02.2025

PineChemical Group OY

Helsinki, Finland

Rosin grade BRT is produced according to GOST 14201-83

Date of loading: 27.02.2025

Container no.:   TKRU4459055

Net weight:        23 200 kgs

| Properties | Test results |
| --- | --- |
| Appearance | Transparent glass-looking substance, partly crystallized |
| Rosin Color | J |
| Ash content, % | 0.008 |
| Impurities, % | 0.005 |
| Softening point, °C | 57.25 |
| Acid number, mg KOH/g | 157.3 |
| Non soaping agents, % | 5.93 |

Conclusion of quality control department:

Product conforms to GOST 14201-83. In all applications of Rosin grade BRT is      the sole responsibility of the buyer to respect and comply with any valid intellectual property rights of third parties.

PineChemical Group OY representative

Natalia Sokolova